## Slide 1: THEORY OF METAL MACHINING
Overview of Machining Technology
Theory of Chip Formation in Metal Machining
Force Relationships and the Merchant Equation
Power and Energy Relationships in Machining
Cutting Temperature

## Slide 2: Material Removal Processes
A family of shaping operations, the common feature of which is removal of material from a starting workpart so the remaining part has the desired shape
Categories:
  Machining – material removal by a sharp cutting tool, e.g., turning, milling, drilling
  Abrasive processes – material removal by hard, abrasive particles, e.g., grinding
  Nontraditional processes - various energy forms other than sharp cutting tool to remove material

## Slide 3
Machining
Cutting action involves shear deformation of work material to form a chip .
As chip is removed, a new surface is exposed
Figure 21.2 ‑ (a) A cross‑sectional view of the machining process, (b) tool with negative rake angle; compare with positive rake angle in (a)

## Slide 4: Why Machining is Important
Variety of work materials can be machined
  Most frequently applied to metals
Variety of part shapes and special geometry features possible, such as:
  Screw threads
  Accurate round holes
  Very straight edges and surfaces
Good dimensional accuracy and surface finish

## Slide 5: Disadvantages with Machining
Wasteful of material
  Chips generated in machining are wasted material, at least in the unit operation
Time consuming
  A machining operation generally takes more time to shape a given part than alternative shaping processes, such as casting, powder metallurgy, or forming

## Slide 6: Machining in the Manufacturing Sequence
Generally performed after other manufacturing processes, such as casting, forging, and bar drawing
  Other processes create the general shape of the starting workpart
  Machining provides the final shape, dimensions, finish, and special geometric details that other processes cannot create

## Slide 7: Machining Operations
Most important machining operations:
  Turning
  Drilling
  Milling
Other machining operations:
  Shaping and planing
  Broaching
  Sawing

## Slide 8
Turning
Single point cutting tool removes material from a rotating workpiece to form a cylindrical shape
Figure 21.3 (a) turning

## Slide 9
Drilling
Used to create a round hole, usually by means of a rotating tool (drill bit) that has two cutting edges
Figure 21.3 ‑ The three most common types of machining process: (b) drilling

## Slide 10
Milling
Rotating multiple-cutting-edge tool is moved slowly relative to work to generate plane or straight surface
Two forms: peripheral milling and face milling
Figure 21.3 ‑ (c) peripheral milling, and (d) face milling

## Slide 11: Cutting Tool Classification
Single-Point Tools
  One cutting edge
  Turning uses single point tools
  Point is usually rounded to form a nose radius
Multiple Cutting Edge Tools
  More than one cutting edge
  Motion relative to work usually achieved by rotating
  Drilling and milling use rotating multiple cutting edge tools.

## Slide 12
Figure 21.4 ‑ (a) A single‑point tool showing rake face, flank, and tool point; and (b) a helical milling cutter, representative of tools with multiple cutting edges

## Slide 13: Cutting Conditions in Machining
The three dimensions of a machining process:
  Cutting speed v – primary motion
  Feed f – secondary motion
  Depth of cut d – penetration of tool below original work surface
For certain operations, material removal rate can be found as
MRR = v f d
  where v = cutting speed; f = feed; d = depth of cut

## Slide 14
Cutting Conditions for Turning
Figure 21.5 ‑ Cutting speed, feed, and depth of cut for a turning operation

## Slide 15: Roughing vs. Finishing in Machining
In production, several roughing cuts are usually taken on the part, followed by one or two finishing cuts
Roughing - removes large amounts of material from the starting workpart
  Creates shape close to desired geometry, but leaves some material for finish cutting
  High feeds and depths, low speeds
Finishing - completes part geometry
  Achieves final dimensions, tolerances, and finish
  Low feeds and depths, high cutting speeds

## Slide 16: Machine Tools
A power‑driven machine that performs a machining operation, including grinding
Functions in machining:
  Holds workpart
  Positions tool relative to work
  Provides power at speed, feed, and depth that have been set
The term is also applied to machines that perform metal forming operations

## Slide 17
Orthogonal Cutting Model
A simplified 2-D model of machining that describes the mechanics of machining fairly accurately
Figure 21.6 ‑ Orthogonal cutting: (a) as a three‑dimensional process

## Slide 18: Chip Thickness Ratio
  where r = chip thickness ratio;
  to = thickness of the chip prior to chip formation;
  And
  tc = chip thickness after separation
Chip thickness after cut is always greater than before, so chip ratio is always less than 1.0

## Slide 19: Determining Shear Plane Angle
Based on the geometric parameters of the orthogonal model, the shear plane angle  can be determined as:
  where r = chip ratio, and  = rake angle

## Slide 20
Figure 21.7 ‑ Shear strain during chip formation: (a) chip formation depicted as a series of parallel plates sliding relative to each other, (b) one of the plates isolated to show shear strain, and (c) shear strain triangle used to derive strain equation

## Slide 21: Shear Strain
Shear strain in machining can be computed from the following equation, based on the preceding parallel plate model:
       = tan( - ) + cot 
where  = shear strain,  = shear plane angle, and  = rake angle of cutting tool

## Slide 22
Figure 21.8 ‑ More realistic view of chip formation, showing shear zone rather than shear plane. Also shown is the secondary shear zone resulting from tool‑chip friction

## Slide 23: Four Basic Types of Chip in Machining
Discontinuous chip
Continuous chip
Continuous chip with Built-up Edge (BUE)
Serrated chip

## Slide 24
Segmented Chip
Brittle work materials (e.g., cast irons)
Low cutting speeds
Large feed and depth of cut
High tool‑chip friction
Figure 21.9 ‑ Four types of chip formation in metal cutting:
(a) segmented

## Slide 25
Continuous Chip
Ductile work materials (e.g., low carbon steel)
High cutting speeds
Small feeds and depths
Sharp cutting edge on the tool
Low tool‑chip friction
Figure 21.9 ‑ Four types of chip formation in metal cutting:
(b) continuous

## Slide 26
Continuous with BUE
Ductile materials
Low‑to‑medium cutting speeds
Tool-chip friction causes portions of chip to adhere to rake face
BUE formation is cyclical; it forms, then breaks off
Figure 21.9 ‑ Four types of chip formation in metal cutting: (c) continuous with built‑up edge

## Slide 27
Serrated Chip
Semicontinuous - saw-tooth appearance
Cyclical chip formation of alternating high shear strain then low shear strain
Most closely associated with difficult-to-machine metals at high cutting speeds
Figure 21.9 ‑ Four types of chip formation in metal cutting: (d) serrated

## Slide 28
Forces Acting on Chip
Friction force F and Normal force to friction N
Shear force Fs and Normal force to shear Fn
  Figure 21.10 ‑
  Forces in metal cutting: (a) forces acting on the chip in orthogonal cutting

## Slide 29: Resultant Forces
Vector addition of F and N = resultant R
Vector addition of Fs and Fn = resultant R'
Forces acting on the chip must be in balance:
  R' must be equal in magnitude to R
  R’ must be opposite in direction to R
  R’ must be collinear with R

## Slide 30: Coefficient of Friction
Coefficient of friction between tool and chip:
Friction angle related to coefficient of friction as follows:

## Slide 31: Shear Stress
Shear stress acting along the shear plane:
where As = area of the shear plane
Shear stress = shear strength of work material during cutting

## Slide 32
Cutting Force and Thrust Force
Forces F, N, Fs, and Fn cannot be directly measured
Forces acting on the tool that can be measured:
  Cutting force Fc and Thrust force Ft
  Figure 21.10 ‑ Forces in metal cutting: (b) forces acting on the tool that can be measured

## Slide 35: Forces in Metal Cutting
Equations can be derived to relate the forces that cannot be measured to the forces that can be measured:
  F = Fc sin + Ft cos
  N = Fc cos ‑ Ft sin
  Fs = Fc cos ‑ Ft sin
  Fn = Fc sin + Ft cos
Based on these calculated force, shear stress and coefficient of friction can be determined

## Slide 36: The Merchant Equation
Of all the possible angles at which shear deformation could occur, the work material will select a shear plane angle  which minimizes energy, given by
Derived by Eugene Merchant
Based on orthogonal cutting, but validity extends to 3-D machining

## Slide 37: What the Merchant Equation Tells Us
To increase shear plane angle
  Increase the rake angle
  Reduce the friction angle (or coefficient of friction)

## Slide 38
Higher shear plane angle means smaller shear plane which means lower shear force
Result: lower cutting forces, power, temperature, all of which mean easier machining
Figure 21.12 ‑ Effect of shear plane angle : (a) higher  with a resulting lower shear plane area; (b) smaller  with a corresponding larger shear plane area. Note that the rake angle is larger in (a), which tends to increase shear angle according to the Merchant equation

## Slide 41: Power and Energy Relationships
A machining operation requires power
The power to perform machining can be computed from:
Pc = Fc v
where Pc = cutting power; Fc = cutting force; and v = cutting speed

## Slide 42: Power and Energy Relationships
In U.S. customary units, power is traditional expressed as horsepower (dividing ft‑lb/min by 33,000)
where HPc = cutting horsepower, hp

## Slide 43: Power and Energy Relationships
Gross power to operate the machine tool Pg or HPg is given by
or
where E = mechanical efficiency of machine tool
Typical E for machine tools =  90%

## Slide 44: Unit Power in Machining
Useful to convert power into power per unit volume rate of metal cut
Called the unit power, Pu or unit horsepower, HPu
or
where MRR = material removal rate

## Slide 45: Specific Energy in Machining
Unit power is also known as the specific energy U
Units for specific energy are typically N‑m/mm3 or J/mm3 (in‑lb/in3)

## Slide 46: Cutting Temperature
Approximately 98% of the energy in machining is converted into heat
This can cause temperatures to be very high at the tool‑chip
The remaining energy (about 2%) is retained as elastic energy in the chip

## Slide 47: Cutting Temperature
Several analytical methods to calculate cutting temperature
Method by N. Cook derived from dimensional analysis using experimental data for various work materials
  where T = temperature rise at tool‑chip interface; U = specific energy; v = cutting speed; to = chip thickness before cut; C = volumetric specific heat of work material; K = thermal diffusivity of the work material

## Slide 48: Cutting Temperature
Experimental methods can be used to measure temperatures in machining
Most frequently used technique is the tool‑chip thermocouple
Using this method, K. Trigger determined the speed‑temperature relationship to be of the form:
T = K vm
  where T = measured tool‑chip interface temperature

## Slide 49: Metal Cutting theory
Plastically deform a material using a hard tool in order to obtain desired physical shape and properties
Very complex phenomena
Essential for high precision; high performance products